## Slide 1: Autumn 2016
FYS4340/FYS9340
Diffraction methods and electron microscopy

## Slide 2
http://www.uio.no/studier/emner/matnat/fys/FYS4340/h16

## Slide 3: Preliminary teaching schedule
Lectures on Tuesdays 09:15-11:00
Exercises and lab on Thursdays 12:15-16:00
  Not every Thursday, will be announced.
  Sometimes an extra lecture
  Nothing planned for this week or next

## Slide 4: Contact info:
Anette Gunnæs: eleonora@fys.uio.no
Sandeep Gorantla: s.m.gorantla@smn.uio.no
Patricia Carvalho: patricia.carvalho@sintef.no
Øystein Prytz: oystein.prytz@fys.uio.no
TEM lab: Phuong D. Nguyen: p.nguyen@fys.uio.no
Prep. lab: Ole Bjørn Karlsen: o.b.karlsen@fys.uio.no
HMS officer: Cecilie Granerød: cecilie.granerød@fys.uio.no

## Slide 5: Diffraction methods and electron microscopy
Williams & Carter. Transmission Electron Microscopy. 2nd ed. Springer, 2009.
In particular parts 1,2, and 3
Various articles and papers (mandatory for PhD students)
Additional suggested reading: Fultz and Howe: Transmission electron microscopy and diffractometry of materials.
Both of these textbooks are available online on the UiO network.

## Slide 6: Curriculum
Instrumentation
  Williams and Carter chapters: 1, 2, 3, 5, 6, 9
Specimen preparation
  Williams and Carter chapter: 10
Diffraction
  Williams and Carter chapters: 11, 12, 13, 16, 18, 19, 20, 21
Imaging
  Williams and Carter chapters: 22, 23, 24, 25, 26, 27, 28
EDS
  Williams and Carter chapters: not clarified yet

## Slide 7: Why electron microscopy?
Many of the properties of a material are determined by its defects
  Precipitates and chemical segregation
  2D defects: Interfaces and planar defects
  1D defects: Dislocations
  0D defects: Interstitials and substitutions
Want to investigate these features on the relevant length scale

## Slide 8: The first electron microscope
Knoll and Ruska, first TEM in 1931
Idea and first images published in 1932
By 1933 they had produced a TEM
with two magnetic lenses which gave
12 000 times magnification.
Ernst Ruska: Nobel Prize in physics 1986
Electron Microscope Deutsches Museum, 1933 model

## Slide 9: The first commercial microscopes
1939 Elmiskop by Siemens Company
1941 microscope by Radio corporation of America (RCA)
  First instrument with stigmators to correct for astigmatism. Resolution limit below 10 Å.
Elmiskop I

## Slide 10: Observations of dislocations and lattice images
1956 independent observations of dislocations by:
Hirsch, Horne and Wheland and Bollmann
-Started the use of TEM in metallurgy.
1956 Menter observed lattice images from materials with large lattice spacings.
1965 Komoda demonstrated lattice resolution of 0.18 nm.
Notes: One exceptions was the work of yada who got crystallographic information from chrysotile fibres

## Slide 11: Menter, 1956

## Slide 12: Use of high resolution electron microscopy (HREM) in crystallography
1971/72 Cowley and Iijima
  Observation of two-dimensional lattice images of complex oxides
1971 Hashimoto, Kumao, Hino, Yotsumoto and Ono
  Observation of heavy single atoms, Th-atoms
Notes: Th-compound supported on a graphite thin crystal film. Bright spots attributed to single Th atoms.

## Slide 13: 1970’s
Early 1970’s: Development of energy dispersive x-ray (EDX) analyzers started the field of analytical EM.
Development of dedicated HREM
Electron energy loss spectrometers and scanning transmission attachments were attached on analytical TEMs.
  Small probes making convergent beam electron diffraction (CBED) possible.

## Slide 14: 1980’s and 90’s
Development of combined high resolution and analytical microscopes.
  An important feature in the development was the use of increased acceleration voltage of the microscopes.
  Field Emission Guns (FEG)
Development of Cs and Cc correction
  Probe and image
Improved energy spread of electron beam
  More user friendly Cold FEG
  Monocromator
2000’s

## Slide 15
  Eric Stach (2008), ”MSE 528 Lecture 4: The instrument, Part 1, http://nanohub.org/resources/3907

## Slide 16: Apertures

## Slide 17: The effect of accelerating the electron
U | k = λ-1 (nm-1) | λ (nm) | m/mo | v/c
1 V | 0.815 | 1.226 | 1.0000020 | 0.0020
10 V | 2.579 | 0.3878 | 1.0000196 | 0.0063
100 V | 8.154 | 0.1226 | 1.0001957 | 0.0198
10 kV | 81.94 | 0.01220 | 1.01957 | 0.1950
100 kV | 270.2 | 0.00370 | 1.1957 | 0.5482
200 kV | 398.7 | 0.00251 | 1.3914 | 0.6953
10 MV | 8468 | 0.00012 | 20.5690 | 0.9988
Relations between acceleration voltage,
wavevector, wavelength, mass and velocity

## Slide 18: The requirements of the illumination system
High electron intensity
  Image visible at high magnifications
Small energy spread
  Reduce chromatic aberrations effect in obj. lens
Adequate working space between the illumination system and the specimen
High brightness of the electron beam
  Reduce spherical aberration effects in the obj. lens
Notes: Has to produce a uniform distribution of electrons on the specimen.
Chromatic aberration skisse
Spherical aberration skisse
Why do we want working space?

## Slide 19: The electron source
Two types of emission sources
  Thermionic emission
    W
    LaB6
  Field emission
    W
    ZrO/W
Cold FEG Schottky FEG

## Slide 20: Thermionic guns
Filament heated to give
Thermionic emission
Tungsten (W)
Lanthanum hexaboride (LaB6)
Filament negative
potential to ground
Wehnelt produces a
small negative bias
Brings electrons to
cross over

## Slide 21: The Field emission gun (FEG)
The principle:
  The strength of an electric field E is considerably increased at sharp points.
  E=V/r
rW < 0.1 µm, V=1 kV → E = 1010 V/m
  Lowers the work-function barrier so that electrons can tunnel out of the tungsten.
Notes: Three main parts and acts as an acceleration triode.
These parameters are interrelated and can be varied to optimize the performance of the gun.
Limited by the the properties of the electron source.

## Slide 22: Electron lenses
Electrostatic
  Require high voltage - insulation problems
  Not used as imaging lenses, but are used in modern monochromators or deflectors
Electromagnetic
  Can be made more accurately
  Shorter focal length
F= -eE
F= -e(v x B)
Any axially symmetrical electric or magnetic field has the properties
of an ideal lens for paraxial rays of charged particles.
Notes: Paraxial rays: rays close to the optcal axis.
Wien filter

## Slide 23: Electromagnetic lens
Bore
Soft Fe pole piece
gap
Cu coil
Current in the coil creates
A magnetic field in the bore.
The magnetic field has axial
symmetry, but is inhomogenious
along the length of the lens.
The soft iron core can increase the field by several
thousand times.

## Slide 24: General features of electromagnetic lenses
Focuses near-axis electron rays with the same accuracy as a glass lens focuses near axis light rays.
Same aberrations as glass lenses.
Converging lenses.
The bore of the pole pieces in an objective lens is about 4 mm or less.
A single magnetic lens rotates the image relative to the object.
Focal length can be varied by changing the field between the pole pieces (changing magnification).
http://www.matter.org.uk/tem/lenses/electromagnetic_lenses.htm