Crystallography revisited

- Are there grain boundaries in amorphous materials?

- Can crystalline solids be isotropic?

- Sketch the  direction and the  plane in an orthorhombic cell.

- Sketch the  direction and the  plane in a monoclinic cell.

- In tetragonal crystals which are

  - the directions of the  form and

  - planes of the  form

- (a). Determine the relation between zone axis indices and Weber indices (expressly defined for hexagonal unit cells)

- Convert the zone axis indices  and  into Weber indices. Convert the  and  Miller indices into Miller-Bravais indices.

- What is the utility of the 4 indices?

Diffraction Questions

- According to the structure factor expression what are the conditions for constructive interference for a body center cubic cell? And for a body center tetragonal cell?

- Fully and consistently index the following diffraction pattern obtained by transmission electron microscopy. The structure is simple cubic with a = b = c = 0.2 nm.

R1 = R2

R2

R1

- Fully and consistently index the following diffraction pattern of Ni obtained by transmission electron microscopy with basis on the expected reflections for a fcc structure. The electron wavelength is 0.002507 nm and the camera constant (L) is 0.869 m.

  - R1 = 1.24 cm, R2 = 1.07 cm

  - R1 = R2 = 1.75 cm

R2

R1

R2

R1

a.                                                                                              b.

a.							b.

4. The following diffraction pattern has been obtained from nanostructured copper. Is the material oxidized?

- Simulate kinematical and dynamical diffractograms for the Co3W phase using a suitable software package.

  - What is the structure type of this phase?

  - Compare the simulated diffractograms of Co3W with Ni3Sn. What are the differences?

  - What is the important difference between kinematical and dynamical diffractograms?

Equations:

Relation between R and L (camera length):

R=L*(1/d)

Angle between (h1k1l1) and (h2k2l2) in the cubic system:

Zone axis of plane of (h1k1l1) and (h2k2l2):

Data: