## Slide 1
MENA 3200 Energy Materials
Materials for Electrochemical Energy Conversion
Fuel cells – Electrolysers - Batteries
Truls Norby

## Slide 2: Overview of this part of the course
What is electrochemistry?
Types of electrochemical energy conversion devices
  Fuel cells, electrolysers, batteries
General principles of materials properties and requirements
  Electrolyte, electrodes, interconnects
  Conductivity
  Catalytic activity
  Stability
  Microstructure
Examples of materials and their properties
  SOFC, PEMFC, Li-ion batteries

## Slide 3: What is electrochemistry?
Redox chemistry – reduction and oxidation
  Example: Homogeneous redox reaction
  2H2 + O2 = 2H2O
Electrochemistry is redox chemistry where reduction and oxidation take place at different locations:
  Cathode: O2 + 4H+ + 4e- = 2H2O | 1
  Anode: 2H2 = 4H+ + 4e- | 1
  Total: 2H2 + O2 = 2H2O
The two locations must thus be connected with pathways for ions and electrons
4H+
2H2
O2
2H2O
R
Proton conducting fuel cell
+
4e-
4e-
4H+
2H2
O2
2H2O
Hydrogen membrane

## Slide 4: Electrochemical energy conversion
Reaction:
  Cathode: O2 + 4H+ + 4e- = 2H2O | 1
  Anode: 2H2 = 4H+ + 4e- | 1
  Total: 2H2 + O2 = 2H2O
If we have different pathways for ions and electrons,
  electrolyte for ions,
  electrodes + wire for electrons,
we can
  extract electrical energy from a spontaneous reaction (e.g. fuel cell or discharging battery),
  supply electrical energy to drive a non-spontaneous reaction (e.g. electrolyser cell or charging battery).
4H+
2H2
O2
2H2O
R
Proton conducting fuel cell
+
4e-
4H+
2H2
O2
2H2O
U
Proton conducting electrolyser
+
4e-

## Slide 5: Electrochemical processes without electrodes
If the ions and electrons go in the same material – a mixed conductor – we cannot get or use electrical energy, but we can for instance get chemical processes, gas separation, or heat.
We may get or use work other than electrical – for instance pumping.
In this course we will however mostly disregard these processes, and concentrate on devices with electrolytes and electrodes.
4e-
4H+
2H2
O2
2H2O
Hydrogen membrane
MOz/2
ze-
Mz+
z/4 O2
Oxidising (corroding) metal
M

## Slide 6: Electrochemical cells
Reduction: A + xe- = Ax- | y
Oxidation: B = By+ + ye- | x
Total: yA + xB = yAx- + xBy+
In text, we often represent cells by a diagram of the type
B | By+ || Ax+ | A
Multiple components in one phase are separated by comma
Phase borders: single lines
Half cell border (salt bridge): double line
Electrode where oxidation takes place is called anode.
Electrode where reduction takes place is called cathode.
Anode Oxidation (both start with vowels)
Cathode Reduction (both start with consonants)
Definition of anode and cathode thus not defined by sign of voltage, but on whether process consumes or releases electrons.
4H+
2H2
O2
2H2O
R
Proton conducting fuel cell
Cathode +
Anode -
Cathode -
Anode +
+
-
4e-
4H+
2H2
O2
2H2O
U
Proton conducting electrolyser
4e-
+
-

## Slide 7: Batteries, fuel cells, and electrolysers
Primary batteries
  Factory charged
  Single discharge
Secondary batteries - accumulators
  Rechargeable
  Multiple discharges and recharges
  All chemical energy stored
“Ternary batteries” – fuel cells
  Fuel continuously supplied from external source
Electrolysers
  Reversed fuel cells
  Fuel generated continuously and stored externally

## Slide 8: Primary battery
Example: “Dry cell”/Alkaline battery. Discharge:
Anode (-): Zn + 2OH- = Zn(OH)2 + 2e-
Cathode (+): MnO2 + H2O + e- = MnOOH + OH-
Electrolyte: KOH

## Slide 9: Secondary battery (rechargeable, accumulator)
Example: Li-ion battery. Discharge:
Anode(-): Li = Li+ + e-
Cathode(+): Li+ + 2MnO2 + e- = LiMn2O4
Electrolyte: Aqueous, polymer, or solid state Li+ ion conductor

## Slide 10: Fuel cell
  Polymer Electrolyte Membrane Fuel Cell (PEMFC):
  Anode(-): 2H2 = 4H+ + 4e-
  Cathode(+): O2 + 4H+ + 4e- = 2H2O
  Solid Oxide Fuel Cell (SOFC)
    If necessary, first reforming of carbon-containing fuels:
    CH4 + H2O = CO + 3H2
  Anode(-): 2H2 + 2O2- = 2H2O + 4e-
  Cathode(+): O2 + 4e- = 2O2-

## Slide 11: Electrolysers
Supplied with low energy H2O (or CO2) and electrical energy
PEM: Produces H2 from H2O
  Cathode(-): 4H+ + 4e- = 2H2
  Anode(+): 2H2O = O2 + 4H+ + 4e-
SOEC: Produces H2 from steam (or syngas CO+H2, or a liquid fuel)
  Cathode(-): 2H2O + 4e- = 2H2 + 2O2-
  Anode(+): 2O2- = O2 + 4e-
Materials otherwise as for fuel cells