## Slide 1
MENA 3200 Energy Materials
Materials for Electrochemical Energy Conversion
Part 3
Materials for SOFCs and PEMFCs
Truls Norby

## Slide 2: Overview of this part of the course
What is electrochemistry?
Types of electrochemical energy conversion devices
  Fuel cells, electrolysers, batteries
General principles of materials properties and requirements
  Electrolyte, electrodes, interconnects
  Conductivity
  Catalytic activity
  Stability
  Microstructure
Examples of materials and their properties
  SOFC, PEMFC, Li-ion batteries

## Slide 3: Solid Oxide Fuel Cells (SOFCs)

## Slide 4: Solid Oxide Fuel Cell (SOFC)
2O2-
2H2
2H2O
O2
R
Solid Oxide Fuel Cell (SOFC)
+
4e-
“oxide” reflects that the electrolyte is an oxide and that it conducts oxide ions
Electrode reactions
  Anode(-): 2H2 + 2O2- = 2H2O + 4e-
  Cathode(+): O2 + 4e- = 2O2-
Operating temperature: 600-1000°C
Fuel: H2 or reformed carbon-containing fuels
Potential advantages:
  Fuel flexibility and tolerance
  Good kinetics – no noble metals needed
  High value heat
Current problems:
  High cost
  Lifetime issues

## Slide 5: Typical SOFC designs
SOFCs for vehicle auxiliary power units

## Slide 6: SOFC electrolyte material requirements
Oxide ion conductivity > 0.01 S/cm
  Film of <10 μm gives <0.1 Ωcm2 of resistance or <0.1 V loss at 1 A/cm2
Ionic transport number >0.99
Gastight
Tolerate both reducing (H2) and oxidising (air/O2) atmospheres
Be compatible with both electrodes (TEC and chemistry)

## Slide 7: Oxide ion conductors
Oxygen vacancies
  Obtained by acceptor dopants
    Y-doped ZrO2 (YSZ), Sc-doped ZrO2
    Gd-doped CeO2 (GDC)
    Sr+Mg-doped LaGaO3 (LSGM)
Disordered inherent oxygen deficiency
    Example: δ-Bi2O3
Oxygen interstitials
    No clearcut examples…

## Slide 8: Y-stabilised zirconia; YSZ
Doping ZrO2 with Y2O3
Stabilises the tetragonal and cubic structures
  Higher symmetry and oxygen vacancy mobilities
Provides oxygen vacancies as charge compensating defects
Oxygen vacancies trapped at Y dopants
8 mol% Y2O3 (8YSZ): highest initial conductivity
10 mol% Y (10YSZ): highest long term conductivity
Metastable tetragonal zirconia polycrystals (TZP) of 3-6 mol% Y2O3 (3YSZ, 6YSZ) gives transformation toughened zirconia – better mechanical properties but lower conductivity
Partially replacing Y with Sc and Yb gives less trapping and better strength

## Slide 9: SOFC anode materials requirements
Electronic conductivity > 100 S/cm
Ionic transport as high as possible to spread the reaction from 3pb to the entire surface
Porous
Tolerate reducing (H2) atmospheres
Be compatible with electrolyte and interconnect (TEC and chemistry)
Catalytic to electrochemical H2 oxidation
For carbon-containing fuels:
  Be moderately catalytic to reforming and catalytic to water shift
  Not promote coking
  Tolerant to typical impurities, especially S

## Slide 10: SOFC anodes: Ni-electrolyte cermet
Made from NiO and e.g. YSZ
NiO reduced in situ to Ni
Porous
All three phases (Ni, YSZ, gas) of approximately equal volume fractions and form three percolating networks.
  Electrons
  Ions
  Gas
In addition, Ni is permeable to H, further enhancing the spreading of the reaction sites
  Electrochemical oxidation of H2 is very fast
Problems
  Mechanical instability by redox and thermal cycles
  Sulphur intolerance
  Too high reforming activity. Tendency of coking
Remedies
  Oxide anodes? (Donor doped n-type conductors)

## Slide 11: SOFC cathode materials requirements
Electronic conductivity > 100 S/cm
Ionic transport as high as possible to spread the reaction from 3pb to the entire surface
Porous
Tolerate oxidising (air/O2) atmospheres
Be compatible with electrolyte and interconnect (TEC and chemistry)
Catalytic to electrochemical O2 reduction
Must tolerate the CO2 and H2O-levels in ambient air
  Too basic materials (high Sr and Ba contents) may decompose under formation of carbonates or hydroxides

## Slide 12: SOFC cathodes: Sr-doped LaMnO3 (LSM)
For example La0.8Sr0.2MnO3 (LSM)
p-type electronic conductor: [SrLa/] = [h.]
Active layer is a “cercer” composite with electrolyte
Porous
All three phases (LSM, YSZ, gas) of approximately equal volume fractions and form three percolating networks.
  Electrons
  Ions
  Gas
In addition, LSM is somewhat permeable to O (by mixed O2- and e- conduction), further enhancing the spreading of the reaction sites
Problems and remedies
  Sensitive to Cr positioning from interconnect; coat interconnect and reduce operating temperature
  Too little mixed conductivity; replace Mn with Co; LaCoO3 has more oxygen vacancies than LaMnO3.

## Slide 13: Tomography of the three percolating phases
G.C. Nelson et al., Electrochem. Comm., 13 (2011) 586–589.

## Slide 14: Anode-supported SOFC membrane electrode assembly (MEA)
T. Van Gestel, D. Sebold, H.P. Buchkremer, D. Stöver, J. European Ceramic Society, 32 [1] (2012) 9–26.

## Slide 15: SOFC interconnect materials requirements
Electronic conductivity > 100 S/cm
Ionic transport number < 0.01 to avoid chemical shortcut permeation
Gas tight
Tolerate both reducing (H2) and oxidising (air/O2) atmospheres
Be compatible with anode and cathode electrode materials (TEC and chemistry)
Mechanical strength

## Slide 16: SOFC interconnects
Ceramic interconnects
  Sr-doped LaCrO3
  p-type conductor: [SrLa/] = [h.]
  Problems:
    Very hard to sinter and machine; expensive
    Non-negligible O2- and H+ conduction; H2 and O2 permeable
Metallic interconnects
  Cr-Fe superalloys, stainless steels; Cr2O3-formers
  Very good electrical and heat conduction
  Mechanically strong
  Problems:
    Oxidation, Cr-evaporation
  Remedies:
    Reduce operation temperature

## Slide 17: Polymer Electrolyte Membrane Fuel Cells (PEMFCs)

## Slide 18: Polymer Electrolyte Membrane (PEM) Proton Exchange Membrane (PEM) PEM Fuel Cell (PEMFC)
Electrode reactions
  Anode(-): 2H2 = 4H+ + 4e-
  Cathode(+): O2 + 4H+ + 4e- = 2H2O
Operating temperature: 80°C
Fuel: Pure H2
Advantages:
  Robust materials
Challenges:
  High cost of membrane and Pt catalyst
  Carbon oxidation
  Low value heat – heat exchange / cooling difficult
  Water management

## Slide 19: Typical PEMFC designs

## Slide 20: PEMFC electrolyte material requirements
Proton conductivity > 0.1 S/cm
Ionic transport number >0.99
Gastight
Tolerate both reducing (H2) and oxidising (air/O2) atmospheres

## Slide 21: Polymer proton conductors
Nafion®
  Perfluorinated backbone
  Grafted
  Sulfonated
  Neutralised by NaOH; Na+
  Proton exchanged; H+
  Swelled with water
  Hydrophobic framework
  Channels with hydrophilic walls
  Protolysis to form H3O+ in the water phase
  Transport of H+ drags ca. 6 H2O molecules
  Backdraft of water

## Slide 22: PEMFC electrode materials requirements
Electronic conductivity
Catalytic activity at largest possible electrode-electrolyte interface
Porous to allow gas access
Tolerate reducing (H2, anode) and oxidising (O2, cathode) conditions

## Slide 23: PEMFC electrode materials and structures
Carbon papers
Graphite
Carbon nanoparticles
Catalyst nanoparticles
Soaked with electrolyte
Porous gas diffusion layer

## Slide 24: PEM electrode materials and structures
Noble metal nanoparticles dispersed on nanostructured carbon supports
Decreases noble metal loading
Challenge: Agglomeration of nanoparticles reduces activity
Challenge: Cathode carbon is oxidised by O2 if no current is drawn.

## Slide 25: PEMFC interconnect materials requirements
Electronic conductivity > 100 S/cm
Ionic transport number < 0.01 to avoid chemical shortcut permeation
Gas tight
Tolerate both reducing (H2) and oxidising (air/O2) atmospheres
Be compatible with electrode and electrolyte materials, notably acidity of electrolyte
Mechanical strength

## Slide 26: PEMFC interconnects
Graphite interconnects
  Pure graphite
  Composites
  Light weight
Metallic interconnects
  Commercial stainless steels
  Very good electrical and heat conduction
  Inexpensive
  Mechanically strong
  Problems:
    Oxidation in contact with electrolyte

## Slide 27: Electrolysers vs fuel cells
In an electrolyser, the product of a fuel cell (H2O, possibly also CO2) is fed…
…the process forced backwards to produce primarily H2 and O2
H2 may in turn reduce CO2 to form CO…
The same materials and structures may be used, but:
  In a fuel cell, the chemical potential gradient is decreased due to losses – less severe materials requirements compared to equilibrium
  In an electrolyser, the chemical potential gradient is increased to overcome the losses – more severe materials requirements compared to equilibrium; more reducing and oxidising conditions